PEROVSKITE RELATED REDUCED VANADIUM OXIDES WITH Pb2+ AND Bi3+ CATIONS IN A-FRAMEWORK

R. Shpanchenko1, A. Belik,2 E. Takayama-Muromachi2, J. Hadermann3, A. Balagurov4
 and E. Antipov1

1 - Department of Chemistry, Moscow State University, Moscow, 119992, Russia; e-mail: shpanchenko@icr.chem.msu.ru

2 - National Institute for Materials Science (NIMS), Tsukuba, 305-0044, Japan

3 - EMAT University of Antwerp (RUCA), Groenenborgerlaan 171, 2020 Antwerp, Belgium

4 - Frank Laboratory JINR, Dubna, 141980, Russia

The magnetoelectric effect implies a coupling between ferroelectricity and magnetic order in the system: the application of an external magnetic field leads to the appearance of an electrical polarization. Pb2+ and Bi3+ are the most suitable A-type cations for search for new multiferroics since they often result in a formation of non-centrosymmetric structures due to a presence of sterically active lone pair. The use of high-pressure high-temperature (HPHT) technique can stabilize perovskite-like compounds with lead and bismuth which could not be obtained at ambient conditions. Such oxides may be good candidates in multiferroic materials.

We prepared Pb1-xMxVO3 solid solutions (where M = alkali or rare earth metal) using HPHT technique. Electron (M3+) or hole (M+) doping leads to a change of the oxidation state of vanadium atoms. As a result a number of structural transformations occurs. Initially tetragonal unit cell successively change the symmetry to cubic and then to orthorhombic ones.

Instead of simple BiVO3 perovskite a new Aurivilius phase, namely Bi4V3O12, was obtained at the similar HPHT conditions. The compound has three polymorph modifications. The room temperature phase has incommensurate modulated structure with the modulation vector q=1/6a* + c* (monoclinic superspacegroup I2/m((0()). The ( component is very small and is observed only as a minor deviation away from the a* axis. In the second phase the ( component has disappeared and the ( component has increased up to q=0.23a*. The reflection condition for the second phase (hklm: h+k+l+m=2n) agrees with the orthorhombic superspacegroup Xmmm((00)000. These modulations are very similar to those found in several Aurivillius compounds containing (BiO)2 double layers.

Презентация ICDD:

БАЗЫ ДАННЫХ ICDD – НОВЫЕ ВОЗМОЖНОСТИ

ICDD DATABASES – NEW POTENTIAL

Не больше 30 мин.

На время конференции будет установлен стенд с материалами ICDD (размер 3.5 х 2.0 м).

Contact information:

# R.V. Shpanchenko

Tel: +7 (495) 939-3490

FAX: +7 (495) 939-4788

E-mail:  Shpanchenko@icr.chem.msu.ru

Inorganic Crystal Chemistry Laboratory, Dept. of Chemistry, Moscow State University, 19992 Moscow, Russia

The preferred presentation type is oral.