High pressure and high temperature carbon isotope fractionation in Fe–C system and its geochemical consequence

Reutsky V.N.

V.S. Sobolev Institute of Geology and Mineralogy SB RAS, Novosibirsk, reutsky@igm.nsc.ru

Carbon forms very few mineral phases in the Earth's mantle at depths exceeding 200 km. The major phases are native carbon (graphite or diamond) and metal (mainly Fe) carbides (Stagno, Frost, 2010). It is widely accepted now that there is a possibility of metal saturation of the mantle below 150 km (Rohrbach et al, 2007; Frost, McCammon, 2008, Dasgupta, Hirschmann, 2010). Therefore, the presence of carbon in association with iron would allow for the formation of iron carbides. Not much is known about relationship of carbon isotope compositions between named phases. Empirical studies of carbon in meteorites show that cohenite ((Fe,Ni,Co)3C) is depleted in 13С relative to graphite from the same meteorite in a range from 0 to 15‰ (Deines, Wickman, 1973; 1975; Newton, Sugiura, 2000). Carbides are also found as inclusions in diamonds (Kaminsky, Wirth, 2011, Smith et al., 2016). Mikhail et al. (2014) have reported 7‰ depletion in 13C of iron carbide inclusions compared to host diamond from the Jagersfontein mine, South Africa.

Looking to the Fe–C phase diagram (Fig. 1) one can see not much possibility for co-crystallization of iron carbides and graphite/diamond from a Fe–C melt within geochemically feasible PTx conditions (Lord et al, 2009). It is possible only within restricted area of peritectic reaction where the L+Fe3C+Dm/Gr association is stable. Early experimental investigation of carbon isotope fractionation in the solid part of the Fe-C phase diagram within the Gr(Dm)+Fe3C and Gr(Dm)+Fe7C3 fields failed to determine the value of isotope fractionation for diamond-carbide pairs because the metastable Fe–Gr eutectic melting, which is approximately 100° lower than the actual Fe-Fe3C eutectic (Strong, Chrenko, 1971). This metastable melting provides carbon re-crystallization via Fe-C melt rather than solid state synthesis of equilibrium diamond and carbide (Reutsky, Borzdov, 2013). On the other hand, extremely slow carbon isotope diffusion in diamond prevents re-equilibration of isotope compositions at solid state conditions.

Figure 1. (a) Iron rich part of the Fe-C diagram at 5 GPa (Lord et al., 2009) modified to show the L+Dm field at 5.5 GPa (Strong, Chrenko, 1971). L – field of Fe-C melt; Gr – graphite; Dm – diamond; Fe – iron; Fe3C and Fe7C3 – corresponding carbides. (b) Particular region of experiments. Open circles – initial compositions of the mixture and first portion of melt Expected change of melt composition is shown with arrows.

In our earlier experiments (Reutsky et al., 2015) we had crystallizing Fe-C melt at 6.3GPa and 1600oC with slow cooling down to 1400oC during 3 hrs. Different initial proportion of iron metal (grade 99,998) and graphite (13CVPDB=-23.0‰) provides crystallization of carbide with or without diamond. After experiments about 20% of Fe-C melt was quenched forming fine iron-carbide aggregate. This allows examination 13C of Fe-C melt from which crystallization took place along with cohenite and diamond crystals.

In carbon-rich compositions diamond crystals were grown first from Fe-C melt at 1600oC within L+Dm stability field. These diamonds had higher 13C values (–20.3 to –22.2‰) than the carbon isotope composition of the starting mixture testifies early crystallization of diamond from Fe-C melt with expected isotope fractionation coefficient (Reutsky et al., 2008). Iron carbide starts to grow later at about 1570oC due to peritectic reaction L+Dm→L+Fe3C. The carbon isotope composition of Fe3C in these experiments changes from -26.2 up to -24.8‰ along direction of growth.

In carbon-poor compositions the L+Dm field was not crossed and no diamond was found. Fe3C aggregates show measurable isotope trends in directions of growth testifies isotope fractionation during cohenite crystallization. However, in this case the trend of 13C in Fe3C aggregate have opposite direction and starts from -24.8 going down to -26.8‰. Direct measurements of 13C of iron carbide and quenched Fe-C melt nearby phase’s boundary reveal 2.00.5‰ enrichment of crystalline phase by 13C isotope in both carbon-rich and carbon-poor experiments.

In terms of carbon isotopes, the peritectic reaction looks like L1+Dm→L2+Fe3C and L1 differs from L2 in carbon isotope ratio by adding heavy isotope from reacting diamond. Bearing in mind twice as much isotope fractionation at diamond growth in comparison with cohenite, both of the trends represent isotope depletion in accordance with Rayleigh’s equations (Reutsky et al., 2015).

Next series of experiments for HPHT crystallization of carbon-poor Fe-C melt using a range of 13CVPDB of initial graphite from -52 up to +39 ‰ show the same relationship of crystalline Fe3C and quenched Fe-C melt. In these series we were applying different cooling rates. The scale of cohenite enrichment in heavy carbon isotope relative to the melt varies from 9.3 to 0.6‰ and correlates with crystallization rate. Experiments with different initial 13C but the same cooling rates give equal scale of carbon isotope fractionation, meaning dominated role of kinetics. SIMS technique reveals pronounced down-trends of 13C values in direction of growth of the crystalline iron carbide regardless of actual 13C/12C value.

Figure 2. Kinetic dependence of carbon isotope fractionation at Fe3C crystallization from Fe-C melt. Black diamonds – 13Ccarbide-13Cmelt values, Open squares – initial 13C compositions of particular experiments.

Difference of carbon isotope composition between diamond and residual melt in our experiments is within 6–7‰ which fits well results of Mikhail et al. (2014) for diamond-carbide inclusion relationship. This similarity can suggest crystallization of sample, investigated by S.Mikhail with co-workers, near the peritectic region of Fe-C diagram.

Documented differences of 13C values between carbide and quenched melt near the crystallization interface along with gradual depletion of Fe3C by heavy carbon isotope indicate selective 13C capture by crystallizing cohenite. Isotope profiles within crystalline Fe3C aggregate also indicate that carbon isotope diffusion does not provide compositional relaxation of isotope heterogeneity under the experimental conditions near the melting point. These observations provide basis for consideration of Fe-C crystallization as one of mechanisms for generation of carbon isotope heterogeneity in the mantle. Crystallization of Fe-C melt in the Earth’s mantle is suggested being responsible for genesis of extra-large diamonds (Smith et al., 2016). If correct, significant amount of iron carbide crystallized from this melt also can present in the mantle. If the melt was able to migrate while crystallize, the last portions of carbide can be significantly depleted in heavy carbon isotope in comparison with initial isotope ratio. This mechanism can be applicable for early Earth differentiation when metal (mainly iron) melts had oozed through the forming silicate mantle. Because carbon is virtually insoluble in minerals (Shcheka et al., 2006), at metal-silicate interface it goes to metal. Thus, significant part of primordial carbon should have gone into the Earth’s core dissolved in metal melts (Dasgupta, 2013, Chi et al., 2014). Some fraction of this carbon has remained in the silicate mantle in the form of accessory phases, including graphite and diamond. Both minerals are heavier in carbon isotope composition compared to Fe-C melt and its crystallization provides depletion of the melt by 13C isotope. Partial crystallization of the metal-carbon melts to carbide leads to further depletion of residual liquid in 13C isotope even at high temperature and high pressure. Accounting potential amount of the melt and carbide, the core-forming metal melts can be extremely isotopically light in comparison with initial carbon isotope ratio. Carbon reservoirs differing in isotope composition could be generated by iron carbide and diamond crystallization during the primary differentiation of the Earth, even if it was initially well-homogenized. The carbon isotope ratio in these reservoirs should significantly lowering with depth. The existence of such reservoirs is widely discussed on the basis of carbon isotope compositions of mantle xenoliths and diamonds (Cartigny, 2010; Deines, 2002; Stachel et al, 2009).

Particular form of carbon depends on the metal/C ratio and metal composition of certain region of the mantle. At depth greater than 250-300 km a Fe-Ni-C melt phase assumed to be present (Rohrbach et al., 2014). The presence of nickel lowers the eutectic temperature of the Fe-C system and blocks the formation of carbides. Therefore, such a composition restricts the occurrence of carbides in the mantle. However, metasomatized crustal slabs low in nickel could be good example for potential source of iron carbides in association with diamond and melts (Rohrbach et al., 2014). On the other hand, nickel, as well as sulfur and silicon, lowers the solubility of carbon in metal melt (Dasgupta et al., 2013, Chi et al., 2014). Increasing pressure with depth decreases carbon solubility in Fe-Ni-C alloy as well (Narygina et al., 2011). At equal metal/C ratio, increasing Ni-content and depth provides an increase in carbon saturation and a lowering of the carbon amount needed for diamond nucleation. In case of sulfur-rich melt the temperature over 1600°C is required for diamond nucleation (Palyanov et al., 2006). Silicon carbide also can occur at great depth, where carbon is depleted in heavy isotope. It can explain systematically low 13C of SiC found in kimberlites (Shiryaev et al., 2008, Trumbull et al., 2009).

Considering the carbon abundance and metal/C ratio, Dasgupta and Hirschmann (2010) have shown that the assemblage of (Fe, Ni) carbide+Fe-Ni metal can be stable from ca. 50 to 500 ppm C at Fe0 contents up to 1wt. %, which corresponds to OIB source mantle. In contrast, the MORB source mantle, with 10-30 ppm C and the same Fe0 content, must hold all of the carbon as light alloying elements in metals. Our data on carbon isotope fractionation provides evidence that iron carbide and carbon-bearing metal must be isotopically distinct carbon reservoirs.

Author is thankful to colleagues helped realization of these studies: Dr. Yury Borzdov, Dr. Yury Palyanov, Marina Kolbasova, Alexander Krupnitskiy, Roman Morozov, Dr. Michael Wiedenbeck. Excellent support of Frédéric Couffignal and Alexander Rocholl during measurements with Cameca 1280-HR at GFZ Potsdam is appreciated. Synthesis of carbide samples was supported by RFBR grant 16-05-00843a. Analytical measurements at SIMS LAB GFZ Potsdam were performed with support of Russian Science Foundation grant № 14-27-00054.

References

Stagno V, Frost DJ (2010) Carbon speciation in the asthenosphere: Experimental measurements of the redox conditions at which carbonate-bearing melts coexist with graphite or diamond in peridotite assemblages. Earth Planet Sci Lett 300: 72–84.

Rohrbach A, Ballhaus C, Golla–Schindler U, Ulmer P, Kamenetsky VS, Kuzmin DV (2007) Metal saturation in the upper mantle. Nature 449: 456–458.

Frost DJ, McCammon CA (2008) The redox state of Earth’s mantle. Annu Rev Earth Planet Sci 36: 389–420.

Dasgupta R, Hirschmann MM (2010) The deep carbon cycle and melting in Earth’s interior. Earth Planet Sci Lett 298: 1–13.

Deines P, Wickman FE (1973) The isotopic composition of graphitic carbon from iron meteorites and some remarks on the troilitic sulfur of iron. Geochim Cosmochim Acta 37: 1295–1319.

Deines P, Wickman FE (1975) A contribution to the stable carbon isotope geochemistry of iron meteorites. Geochim Cosmochim Acta 39: 547–557.

Newton J, Sugiura N (2000) Carbon isotope measurements in iron meteorites. Meteorit Planet Sci 35: A118.

Kaminsky FV, Wirth R (2011) Iron carbide inclusions in lower-mantle diamond from Juina, Brazil. Canad Min 49: 555-572.

Smith EM, Shirey SB, Nestola F, Bullock ES, Wang J, Richardson SH, Wang W (2016) Large gem diamonds from metallic liquid in Earth’s deep mantle. Science 354(6318): 1403-1405.

Mikhail S, Guillermier C, Franchi IA, Beard AD, Crispin K, Verchovsky AB, Jones AP, Milledge HJ (2014) Empirical evidence for the fractionation of carbon isotopes between diamond and iron carbide from the Earth's mantle. Geochem Geophys Geosystems 15(4): 855-866.

Lord OT, Walter MJ, Dasgupta R, Walker D, Clark SM (2009) Melting in the Fe–C system to 70 GPa. Earth Planet Sci Lett 284: 157–167.

Strong HM, Chrenko RM (1971) Properties of Laboratory-Made Diamond. J Phys Chem 76: 1838-1843.

Reutsky VN, Borzdov YuM (2013) A comment on “Experimental determination of carbon isotope fractionation between iron carbide melt and carbon: 12C-enriched carbon in the Earth's core?” by M. Satish-Kumar, H. So, T. Yoshino, M. Kato, Y. Hiroi [Earth Planet. Sci. Lett. 310 (2011) 340–348]. Earth Planet Sci Lett 368: 219–221.

Reutsky VN, Borzdov YM, Palyanov YN (2015). Carbon isotope fractionation during high pressure and high temperature crystallization of Fe–C melt. Chem Geol 406: 18-24.

Reutsky VN, Borzdov YM, Palyanov YN (2008) Carbon isotope fractionation associated with HPHT crystallization of diamond. Diam Relat Mater 17: 1986-1989.

Shcheka SS, Wiedenbeck M, Frost DJ, Keppler H (2006) Carbon solubility in mantle minerals. Earth Planet Sci Lett 245: 730–742.

Dasgupta R (2013) Ingassing, storage, and outgassing of terrestrial carbon through geologic time. Rev Min Geochem 75: 183–229.

Chi H, Dasgupta R, Duncan MS, Shimizu N (2014) Partitioning of carbon between Fe-rich alloy melt and silicate melt in a magma ocean – Implications for the abundance and origin of volatiles in Earth, Mars, and the Moon. Geochim Cosmochim Acta 139: 447–471.

Cartigny P (2010) Mantle-related carbonados? Geochemical insights from diamonds from the Dachine komatiite (French Guiana). Earth Planet Sci Lett 296: 329–339.

Deines P (2002) The carbon isotope geochemistry of mantle xenoliths. Earth-Sci Rev 58: 247–278.

Stachel T, Harris JW, Muehlenbachs K (2009) Sources of carbon in inclusion bearing diamonds. Lithos 112: 625.

Rohrbach A, Ghosh S, Schmidt MW, Wijbrans CH, Klemme S (2014) The stability of Fe–Ni carbides in the Earth’s mantle: Evidence for a low Fe–Ni–C melt fraction in the deep mantle. Earth Planet Sci Lett 388: 211–221.

Narygina O, Dubrovinsky LS, Miyajima N, McCammon CA, Kantor IYu, Mezouar M, Prakapenka VB, Dubrovinskaia NA, Dmitriev V (2011) Phase relations in Fe–Ni–C system at high pressures and temperatures. Phys Chem Minerals 38: 203–214.

Palyanov YuN, Borzdov YuM, Khokhryakov AF, Kupriyanov IN, Sobolev NV (2006) Sulfide melts–graphite interaction at HPHT conditions: Implications for diamond genesis. Earth Planet Sci Lett 250: 269–280.

Shiryaev AA, Wiedenbeck M, Reutsky V, Polyakov VB, Mel’nik NN, Lebedev AA, Yakimova R (2008) Isotopic heterogeneity in synthetic and natural silicon carbide. J Phys Chem Solids 69(10): 2492-2498.

Trumbull RB, Yang JS, Robinson PT, Di Pierro S, Vennemann T, Wiedenbeck M (2009) The carbon isotope composition of natural SiC (moissanite) from the Earth's mantle: New discoveries from ophiolites. Lithos 113(3): 612-620.